STATUTORY ULTRASONIC THICKNESS SURVEY REPORT

NON-DESTRUCTIVE TESTING LABORATORY - API 510 / ASME SECTION V

Report No: NDT/HCU/2026/UT-9021 | Date: 04-Sep-2026

Unit: Hydrocracker (HCU-11) | Equipment: HP Separator (11-V-102)

Base Metal: SA-387 Gr 22 Cl 2 (2.25Cr-1Mo) | Nominal Thickness: 145.0 mm | Code Min (t_min): 138.57 mm

1. Ultrasonic C-Scan Grid Readings

Point TH-01 (Top Head Crown): 139.60 mm (Loss: 0.60 mm, Rate: 0.05 mm/yr) - ACCEPTABLE

Point SC-1A (Shell C-1 0 deg N): 142.40 mm (Loss: 2.70 mm, Rate: 0.20 mm/yr) - ACCEPTABLE

Point SC-2A (Shell C-2 90 deg E): 141.20 mm (Loss: 4.00 mm, Rate: 0.325 mm/yr) - MONITOR

Point BK-01 (Bottom Knuckle Impingement): 138.20 mm (Loss: 6.80 mm, Rate: 0.75 mm/yr) - CRITICAL BREACH

2. Defect Finding & Remaining Life

Point BK-01 measured thickness (138.20 mm) has BREACHED code minimum allowable (138.57 mm) by -0.37 mm.

Remaining service life per API 510 Section 7.1.1 is -0.49 Years (EXPIRED).

HTHA micro-fissuring indications detected on longitudinal weld seam L-1.

3. Statutory Disposition & Mandatory Action

1. IMMEDIATE DERATING: Operating pressure derated from 145 barg to 118 barg.

2. EMERGENCY APPROVAL NOTE: Initiate Note for Approval for 347 SS weld overlay restoration (Estimated: ₹88 Lakhs).